IMPORTANT

REQUIREMENTS FOR SPECIFICATION LOT TESTING

In compliance with specification requirements for jobs requiring certification, lot testing is performed on all jobs per the requirements of the respective specification.  We at Aotco, as the supplier, require the use of coupons, (4) - 1 x 4 x 0.40, of the same material or similar alloy as the parts to be run with the job.  Coupons will be used when permitted by specification and will be of the material and condition as required by specification.

If lot testing is required by the specification(s) you are requiring, please indicate specific testing needed on your purchase order and be sure to include coupons of the same material or similar alloy as your parts.

Except Copper Sulfate and Water Immersion testing for Passivation can be performed on actual parts in house, when permitted by specification. In recent months Aotco has performed many internal Audits to verify Aotco’s cost of performing all of the tasks that are required by various specifications. One of the largest time consuming task is the required thickness readings. For instance Mil-A-8625 type 3 only, requires eight thickness measurements per sample per AQL

For example 1000 pc job requirement has been General inspection Level 2, sample size 80 pieces, measured 8 times per piece will be 640 thickness measurements, 500 piece job sample size will be 50 pieces measured 8 times per piece will be 400 thickness measurements. As you can see this has been a huge man power cost for Aotco. The same requirement is also for other plating requirements.

In light of the economic times Aotco can either continue and charge accordingly or ask that you sign a waiver for this requirement of all the specifications that would require this type of thickness checks.

Aotco is still obligated to meet the actual thickness requirement per each specification required.

This will avoid a delay to your order until we receive the coupons or this waiver.

If you prefer to waive lot testing, please indicate the specific lot test per specification below. Complete the information below and return this form to us as soon as possible.  This waiver is needed for our files before we can waive any lot testing, on any order. This form will be updated yearly.

Please Fax to 978 670 2441 or email to: ttaylor@aotco.com

Thank you for your understanding.

Sincerely,

Tracy Taylor

Customer Service Representative

WAIVER OF LOT TESTING

This waiver applies to:

- All Orders

- Single order – enter PO# ________________________________________

Part #(s): _____________________________________ Rev: _______________

*Specification(s): ___________________________________________________

Specific Lot test(s):_________________________________________________

Prime Contractor: _________________________________________________

Company Name: __________________________________________________

Contact Name (print):_______________________________________________

Signature: ________________________________________________________

Date: __________ Email Address: ____________________________________